| Tech Data Sheet DMI-3850 |  |
| --- | --- |

Description

DMI-3850 is a proprietary, UV-curable adhesive specially designed for space applications with a need for low/no VOC content and virtually no outgassing. DMI-3850 contains no photoinitiators or polymerization inhibitors that can contribute to weight loss issues.

In its cured state DMI-3850 is a soft and rubber-like solid and is suitable for a number of applications.

## Highlights

Clear and colorless to light yellow

UV curable

Suitable for low stress applications Low VOC content

## Typical Physical and Chemical Properties

| PROPERTY | METHOD | RESULT |
| --- | --- | --- |
| Appearance at Room Temperature | Visual | Clear and colorless to light yellow viscous liquid |
| Viscosity @ 60°C (typical) | Haake Rheometer | 45 kcP |
| Weight loss @ 200ºC (typical – neat) | TGA | < 0.2 % |
| Flash Point | Closed Cup | > 200°C |
| Recommended Storage Temp |  | Room Temperature |

Data is for reference only and may vary depending on testing method used.

Recommended Formulation Use:

DMI-3850  is recommended for use as an adhesive in applications demanding low VOC and outgassing (e.g. space).  DMI-3850 is self-reactive and does not require the use of a photoinitiator for UV curing. The amount of UV energy required to fully cure the material must be determined by the customer.

Since the curing rate of DMI-3850 is slower than typical photoinitiator-cured materials it is suggested that curing take place in an air inhibited environment (e.g. inert gas atmosphere, between glass plates, etc.)

Contact:

REQUEST A SAMPLE OR PLACE AN ORDER

Customer Support ( 858-348-1122 ( support@designermoleculesinc.com REF: DMI Part Number: R1429